## Slide 1
Ossy Siegmund, Sharon Jelinsky, Jason McPhate, Joe Tedesco
Experimental Astrophysics Group,
Space Sciences Laboratory,
U. California at Berkeley
Progress with Bialkali Photocathode Development

## Slide 2
Biakali Cathode - Configurations
Photocathode Operation Schemes
Nominal Cherenkov emission spectrum compared with bialkali
Bialkali is a few 100Å thick, and is nominally a deposition as a semitransparent layer on the window, with a proximity gap to the first MCP.

## Slide 3
6*109Ohm/square
2*106Ohm/square
Typical Bi-Alkali Cathode Characteristics
QE and resistivity for various bialkali’s We will use Na2KSb – Why? Resistivity,
noise, temperature robustness, uniformity.
Lyashenko, Chicago 7/09
Cathode Noise vs Temp expect 10,000 to 40,000 events/sec for 8” tube bialkali!

## Slide 4
Window of choice B33 - General Parameters
B33 Composition
Refractive index @400nm
B33 1.47
Air ~1.0
Water ~1.32
The cathode substrate, window or window coating, affects the photocathode performance. Borofloat B33 Borosilicate has been
tested, and it is a good photocathode substrate. BUT - it has Tin
diffused into one side, so we polish it. Anti-reflection coatings
not baselined, (5 to 9% reflectance in bandpass).
Samples coated by Joe Libera, measured by Lisa Pawlowicz
B33 Transmittance is typical of boro-silicate glasses. We have found no good under-layers yet. Will try MnO.

## Slide 5: Bialkali Cathode Development Program
Small window cathode development, 1.22” samples, 4 per run
  Process samples to optimize QE and bandpass
    Study Na2KSb, K2CsSb cathodes
  Used several substrate materials, SiO2, verified B33
  Tested MgO/ITO/conductor underlayer for cathodes
Large size window cathode study, 8.7” windows.
  Developed source alkali design for large cathodes
  Developing techniques to make larger area uniform QE
  Optimization cathode QE levels started
  Decide if metal conductor underlayer is needed
  Test window metalization and sealing techniques
Notes: The sensitivity of the activated photocathode is considerably higher, with a quantum efficiency of as high as 37% at about 450 Å and a sensitivity cut off energy of about 6.2 eV. The observed decrease of sensitivity at 988 and 520 Å (and probably not observed at ~670 Å) is likely to correspond to 2xEgap+Eaff,, 4xEgap+Eaff,, and 3xEgap+Eaff,, respectively. A much better spectral continuity of the illumination source is required in order to study the UV absorption fine structure.

## Slide 6
Work Flow Program for Bialkali
Cathode Development
We have
run all the processes. Now we need to optimize the 20cm depositions.

## Slide 7
7
Tube Lab, 1.2” old sample test/process station.
Small tank used to process alkali cathodes (33mm) and tubes of small area. Can take 4-8 samples/run. 7 runs done, more than 30 substrate coatings.
Small sample test runs
Substrate material tests

## Slide 8: Bialkali Cathode Process Development Program
We cut up 8.7” B33 windows to make ~50 ea 1.22” test samples. Inconel annular electrodes were evaporated just as they would be for In seals
Window holder inside tank
Window holders and mask
Small window cathode development, 1.22” samples
  Processed samples to optimize QE and bandpass
Notes: The sensitivity of the activated photocathode is considerably higher, with a quantum efficiency of as high as 37% at about 450 Å and a sensitivity cut off energy of about 6.2 eV. The observed decrease of sensitivity at 988 and 520 Å (and probably not observed at ~670 Å) is likely to correspond to 2xEgap+Eaff,, 4xEgap+Eaff,, and 3xEgap+Eaff,, respectively. A much better spectral continuity of the illumination source is required in order to study the UV absorption fine structure.

## Slide 9: Bialkali Photocathode Sample Tests
Bialkali test cathodes made on polished 31mm B33 windows gave the best results. The KCsSb does not perform as well as Na2KSb in the transfer cathode situation expected for the 8” tubes. Na2KSb hot, right after deposition, also improves after cool down.
Cathode test runs with KCsSb and Na2KSb cathodes on borofloat-33 windows. Na2KSb >20% QE achieved, QE uniformity better than ± 15%.

## Slide 10
  Cathode run #6B, Na2KSb Uniformity
842
845
822
848
839
  B33 substrate, 1” aperture, 395nm light, QE uniformity is good

## Slide 11: Cathode/Substrate Materials Summary
  ITO and MgO, 5nm are QE are deficient
  No problems with inconel evaporated borders good adhesion/conduction
  K2CsSb cathode fabrication is problematic, lower temp
  non-uniformity, less stability, poor conductivity, more noise.
  B33 is a good substrate material
  Going to try MnO (ALD, and sputtered) as underlayer to enhance QE
  Work with Na2KSb as baseline, Inconel stripes if needed, arranged on same “X” as support. OK for rigorous cleaning, high temp, stable, uniform, high conductivity, good QE.
Notes: The sensitivity of the activated photocathode is considerably higher, with a quantum efficiency of as high as 37% at about 450 Å and a sensitivity cut off energy of about 6.2 eV. The observed decrease of sensitivity at 988 and 520 Å (and probably not observed at ~670 Å) is likely to correspond to 2xEgap+Eaff,, 4xEgap+Eaff,, and 3xEgap+Eaff,, respectively. A much better spectral continuity of the illumination source is required in order to study the UV absorption fine structure.

## Slide 12: 8” Cathode Process Development
Large window cathode development, 8.7” square
  Commissioned 8” cathode/window seal process tank
  Objectives:-
  Repeat small sample depositions for verification
  Verify alkali sources for large cathode areas
  Confirm 8” wet cleaning and plasma cleaning processes
  Test metal stripe/MnO underlayers for cathodes
  Develop techniques to make 8” area uniform QE
  Optimize cathode QE levels and test stability and uniformity
  Trial window seals on 8.7” “frames”
  Then:-----
  Transfer techniques to large tube processing station
Notes: The sensitivity of the activated photocathode is considerably higher, with a quantum efficiency of as high as 37% at about 450 Å and a sensitivity cut off energy of about 6.2 eV. The observed decrease of sensitivity at 988 and 520 Å (and probably not observed at ~670 Å) is likely to correspond to 2xEgap+Eaff,, 4xEgap+Eaff,, and 3xEgap+Eaff,, respectively. A much better spectral continuity of the illumination source is required in order to study the UV absorption fine structure.

## Slide 13: 8.7” Photo-Cathode / Seal test Chamber
8.7” Square PC/seal test process chamber with 14” Dia. Capability 16.5” Dia. Chamber on exact same process cart as the previous chamber.
All-Metal Valves
Ion Pump Port
16.5” Flange Chamber Access
Forming Well - 6”
Larger 16” flange tank, to test
  Quantum efficiency
  QE Uniformity
  Seal tests
Alkali sources

## Slide 14: 8.7” Photo-Cathode / Seal test Chamber
Final assembly done, spent 3 weeks in initial cleanup bakeout up to 375°C to get the chamber conditioned.
Used SAES alkalis & SbPt beads. Employed old source flange to verify process, then move to new larger sources
and flange for next run.

## Slide 15
Preparation of 8.7” B33 Windows for Cathodes
All the tooling is in place. We have wet cleaned, plasma cleaned, and evaporated NiCr on a window, and loaded into the holder for photocathode processing.
Plasma cleaning
NiCr electrode border on B33

## Slide 16: 8” Photocathode First Process, System Load
8.7” window loaded
Final window adjustments

## Slide 17: Photocathode Preparation and Deposition
Alkali / Sb sources in action
Outgassing of SAES Alkalis
Na
K

## Slide 18: Photocathode Deposition
Na
K
K
Sb
Sb

## Slide 19: First 8” 7.5” Bialkali Photocathode
Photocathode Process
82
82
82
82.5
83
79
81
79
81
Relative %
transmission
of PC vs
position
(~corrected for
window transmission)
8”
Uniformity is good
Extra flange to couple alkali flange increased distance and caused vignetting of the deposition. No proper contact with cathode! Fix and repeat!

## Slide 20: 8in Photocathode First Try
8” PC/Seal Test Chamber
  <10-9 Torr base vacuum, RGA operational, fully baked
Chamber configured for 8in depositions
5mm thick, 8.7” polished B33 window
  NiCr border electroded
Deposited Na2KSb photocathode
RGA record for entire process
Very good first run – BUT cathode not big enough – only 7.5”, lots of useful data